# 07 8100 	SPRAYED–ON FIREPROOFING

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of post-consumer/post-industrial recycled content in sprayed-on fireproofing. Additional considerations related to product emissions, product toxicity, or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This section includes sprayed-on fireproofing which meet specified criteria for post-consumer and/or post-industrial recycled content.

  - REFERENCES / QUALITY ASSURANCE

(for recycled content and other High Performance building criteria)

- Recycled content:

- EPA Comprehensive Procurement Guidelines, www.epa.gov/cpg (see insulations).

- Emissions:

- ASTM E 859, Test Method for Air Erosion of Sprayed Fire-Resistive Materials (SFRMs) Applied to Structural Members.

1.03	SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of recycled content per section 2.01 of this specification.

- Manufacturer’s certification of product compliance with emissions testing standards per section 2.01 of this specification (optional).

- Material Safety Data Sheets.

- Manufacturer’s maintenance instructions.

- Manufacturer’s policy statement on sprayed-on fireproofing recycling programs.

1.04	DELIVERY AND STORAGE

- Store materials per manufacturer’s recommendations for allowable temperature and humidity range. Material shall not be allowed to become damp prior to installation.

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmental Criteria:

- Recycled Content:

Sprayed-on fireproofing shall contain a minimum of 75% (combined) post-industrial/post-consumer recycled content. The percentage of recycled content is based on the weight of the component materials.

- Emissions (The following criteria are optional, to be met where feasible):

- In areas subject to impact or vibration (e.g., mechanical rooms), medium density (min. 22 lbs/cf) or high density (( 40 lbs/cf) fireproofing products shall be specified.

- Fungal Resistance: The fireproofing material shall be formulated at the time of manufacturing with a mold inhibitor. Fireproofing material shall be tested in accordance with ASTM G-21 and shall show resistance to mold growth for a period of 28 days for general use and 60 days for materials to be installed in plenums.

PART 3 –  EXECUTION

3.01	INSTALLATION

- Comply with manufacturer’s recommended installation procedures to minimize occupant exposure to dusts and particulates from fireproofing installation.

- Comply with manufacturer’s recommendations for space ventilation during and after fireproofing installation.

3.02	WASTE MANAGEMENT

- Identify manufacturer’s policy for collection or return of construction scrap, unused material, and/or packaging material. Where feasible, institute construction waste separation and recycling to take advantage of manufacturer’s programs.

END OF SECTION 07812