# 09 3000 	CERAMIC TILE

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of post-consumer/post-industrial recycled content in ceramic tile. Additional considerations related to product emissions, product toxicity, or other High Performance building criteria are included where appropriate.

PART 1 - GENERAL

1.01  SUMMARY

- This section includes ceramic, glass, and ceramic/glass composite tiles which meet specified criteria for post-consumer and/or post-industrial recycled content.

  - REFERENCES / QUALITY ASSURANCE

(for recycled content and other High Performance building criteria)

- Adhesives:

“Green Seal Environmental Standard for Certification of Commercial Adhesives” (GS-36),

Green Seal, Inc., Washington, DC, http://www.greenseal.org

1.03	SUBMISSION REQUIREMENTS

A	Manufacturer’s certification of recycled content per section 2.01 of this specification.

B.	Manufacturer’s certification of lead-free glazings (for glazed tiles) per section 2.01 of this specification.

- Manufacturer’s certification of product compliance with adhesive standards per section 2.01 of this specification (for mastic-set applications).

- Manufacturer’s certification of product compliance with VOC limits for mortars and grouts per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance and cleaning instructions.

- Manufacturer’s policy statement on ceramic tile recycling programs.

PART 2 – PRODUCTS

2.01 MATERIALS

- Environmental Criteria:

- Recycled Content:

Ceramic, glass, ceramic/glass composite, and terrazzo-type tiles shall contain a minimum of 50% (combined) post-industrial/post-consumer recycled content. The percentage of recycled content is based on the weight of the component materials.

- Hazardous Materials Content:
Glazings used for glazed tiles shall be lead-free.

- Adhesives:

Tile adhesives in mastic-set applications shall meet the VOC limits and prohibited chemical limitations of the “Green Seal Environmental Standard for Certification of Commercial Adhesives” (GS-36), of Green Seal, Inc., Washington, DC.

- Mortars/Grouts:

The VOC content of mortars or grouts for ceramic tile installations shall not be in excess of 150 grams/liter, less water and less exempt compounds.

PART 3 –  EXECUTION

3.01	WASTE MANAGEMENT

- Identify manufacturer’s policy for collection or return of construction scrap, unused material, demolition scrap, and/or packaging material. Where feasible, institute demolition and construction waste separation and recycling to take advantage of manufacturer’s programs.

END OF SECTION 09310