# 09 9000 	VOLATILE ORGANIC COMPOUND (VOC) LIMITS FOR PAINTS

FINAL:  	Feb. 12, 2009

Note:  The following specification criteria have been assembled to promote the procurement of reduced-emission paint products. Additional considerations related to product toxicity or other High Performance building criteria are included where appropriate.

PART 1 – GENERAL

1.01  SUMMARY

- This Section includes requirements for reduced emission, reduced toxicity interior paints (primers & top coats) and anti-corrosive paints for metal in interior applications.

  - REFERENCES / QUALITY ASSURANCE

(for indoor air quality and toxicity criteria)

A.	“Green Seal Environmental Standard for Paints” (GS-11), Green Seal, Washington, DC, www.greenseal.org

B.	“Green Seal Environmental Standard for Anti-Corrosive Paints (GC-03), Green Seal, Washington, DC, www.greenseal.org

1.03 SUBMISSION REQUIREMENTS

A.	Manufacturer’s certification of product compliance with paint standards (VOC content and prohibited compounds) per section 2.01 of this specification.

- Material Safety Data Sheets.

- Manufacturer’s maintenance and cleaning instructions.

1.04	DELIVERY AND STORAGE

- To the extent feasible, do not store paint products with materials that have a high capacity to adsorb VOC emissions (i.e., materials which are woven, fibrous or porous in nature, such as acoustical ceilings, carpet, textiles, etc.). Do not store paint products in occupied spaces.

PART 2 – PRODUCTS

2.01 MATERIALS

A.	Environmentally-Preferable Product Criteria:

1.	VOC Content of Paints:

The volatile organic compound (VOC) content of interior paints, interior primers, and anti-corrosive paints used in interior applications shall not exceed the limits defined in the Green Seal Environmental Standards for Paints (GS-11, dated 5/20/93) and Anti-Corrosive Paints (GC-03, dated 1/7/97), of Green Seal, Washington, DC. The VOC limits defined in the referenced Green Seal standards are as follows. All VOC limits are defined in grams per liter, and exclude water and tinting color added at the point of sale (as determined by U.S. EPA Reference Test Method 24).

| ## Interior Paints & Primers |  | ## Anti-Corrosive Paints |  |
| --- | --- | --- | --- |
| Non-flat: | 150 | Gloss: | 250 |
| Flat: | 50 | Semi-gloss: | 250 |
|  |  | Flat: | 250 |

2. 	Additional Chemical Component Restrictions in Paints:

To the extent feasible, interior paints, interior primers, and anti-corrosive paints used in interior applications shall comply with the following chemical component restrictions of the Green Seal Environmental Standards for Paints (GS-11, dated 5/20/93) and Anti-Corrosive Paints (GC-03, dated 1/7/97), of Green Seal, Washington, DC.

- Aromatic Compounds: the product must contain no more than 1.0% by weight of the sum total of aromatic compounds. Testing for the concentration of these compounds will be performed if they are determined to be present in the product during a materials audit.

b) 	Other Chemicals: the manufacturer shall demonstrate that the following chemical compounds are not used as ingredients in the manufacture of the product.

- Halomethanes: methylene chloride

- Chlorinated ethanes: 1,1,1-trichloroethane

- Aromatic solvents: benzene, toluene (methylbenzene), ethylbenzene

- Chlorinated ethylenes: vinyl chloride

- Polynuclear aromatics: naphthalene

- Chlorobenzenes: 1,2-dichlorobenzene

- Phthalate esters: di (2-ethylhexyl) phthalate, butyl benzyl phthalate, di-n-butyl phthalate, di-n-octyl phthalate, diethyl phthalate, dimethyl phthalate

- Miscellaneous semi-volatile organics: isophorone

- Metals and their compounds: antimony, cadmium, hexavalent chromium, lead, mercury

- Preservatives (antifouling agents): formaldehyde

- Ketones: methyl ethyl ketone, methyl isobutyl ketone

- Miscellaneous volatile organics: acrolein, acrylonitrile

PART 3 –  EXECUTION

3.01	INSTALLATION

- Comply, at minimum, with paint manufacturer recommendations for space ventilation during and after installation. Where feasible, the following ventilation conditions shall be maintained during the paint curing period, or for 72 hours after application: 1) supply 100% outside air 24 hours a day; 2) supply airflow at a rate of 6 air changes per hour, when outside temperatures are between 55 degrees F and 85 degrees F and humidity is between 30% and 60%; and 3) supply airflow at a rate of 1.5 air changes per hour, when outside air conditions are not within the range stipulated in item 2 above.

B.	To the extent practical, allow paint installations to cure prior to the installation of materials that adsorb VOCs. Materials that adsorb VOCs include carpets, textiles, and acoustical ceiling panels.

END OF SECTION 09900