## Slide 1: Storm Water Filter Design --Updates on Filter materials for N removal
Xinwei Mao, Ph.D
Civil Engineering Department, Stony Brook University
New York State Center for Clean Water Technology
Feb 15, 2024

## Slide 2: Outline
Background
Stormwater Infiltration System
Filter design and performance

## Slide 3: Onsite wastewater problem---- Long Island
Kinney and Valiela, 2011
~510,000 conventional onsite wastewater treatment systems (OWTS).
SBU
Notes: A previous study indicated the N sources to the Great South Bay. Septic system is the major N source.
Current OWTSs comprises a septic tank and a following leaching ring. The leaching pool is made of concrete with holes on the side, and no bottom. Such septic systems removes little N and a limited level of Carbon.
Therefore, it is critical for us to upgrade these systems to sustainably and effectively removing N. And this is one of the essential goals of the center. On the other hand, we are also eager to understand how much of the N loading is from legacy N. Especially considering the shallow water table and the depth of the leaching pools.

## Slide 4
Engineered Nitrogen
Removing Biofilter
Nitrification sand layer overlying denitrification lignocellulose layer.
80 – 90% N removal.
Low maintenance demand.
Engineered system which simulate the configuration and process of natural wetland.
20 – 75% N removal.
Ilyas and Hullebusch., 2020
Bioretention system
Background
New York State Center for Clean Water Technology
Onsite Wastewater
Stormwater
Passive filtration
Remove contaminants
Nutrients
Metals
Micropollutants
Low-cost, sustainable

## Slide 5: Outline
Background
Stormwater Infiltration System
Filter design and performance

## Slide 6: Stormwater Infiltration -- Overview
https://urbanwater.melbourne.vic.gov.au/industry/treatment-types/stormwater-and-rainwater-harvesting/

## Slide 7: Contaminants in Stormwater
Nutrients
Metals
Metals
Pathogens
Micro-pollutants

## Slide 8: Stormwater filtration Configuration (example)
Pilot-scale testing of stormwater filtration system

## Slide 9: Stormwater Filter Design
Engineered geomedia
  Carbonaceous materials (biochar)—organic & metal
  Manganese oxide-coated sands —organics & metal
  Woodchips and iron filings —nitrate & phosphate
Location (source, bioretention)
Configuration (unit, combination)
Hydraulics (long-term operation)
Field
(validate, monitoring, longevity)
Pilot
(continuous flow)
Bench
(proof-of concept)

## Slide 10: Outline
Background
Stormwater Infiltration System
Filter design and performance
  Contamination levels in first flush
  Filter design and test

## Slide 11: Stormwater filtration—first flush
https://urbanwater.melbourne.vic.gov.au/industry/treatment-types/stormwater-and-rainwater-harvesting/
“First Flush”: refers to the first few minutes or hours of a storm. The common perception is that during this initial time, the concentration of pollutants in the runoff is greater than during later parts of the storm.

## Slide 12: First Flush sampling during a storm
sample (A)
Samples
B-1
B-2
B-3
B-4
The first-flush storm water was collected at several locations in Stony Brook University.
Notes: The concentrations of contaminants are much higher in the initial portions of the storm water. And the contaminants concentrations will decrease as the collected storm water volume increases.

## Slide 13
Sample Name | Volume (ml) | TSS (mg/L) | COD (mg/L) | TKN (mg-N/L) | pH | Total coliform (MPN/ 100 mL)
A | 500 ml | 230 | 298 | 12.3 | 6.75 | 9200
B-1 | 200 ml | 2760 | 320 | 25.5 | 6.50 | -
B-2 | 1 L | 780 | 139.3 | 1.85 | 6.93 | -
B-3 | 1 L | 470 | 123.9 | 1.80 | 7.06 | -
B-4 | 1 L | 725 | 81.2 | 0.716 | 7.16 | -
Concentrations of contaminants in collected storm water
*a time-course samples were collected at site B (parking lot)
** TSS: total suspended solids (indicator of inorganic/organic contaminants)
COD: chemical oxygen demand (indicator of organic contaminants)
TkN: total keljdel nitrogen (indicator of nutrients for eutrophication)
The first-flush storm water contains the highest level of contaminants (comparable to that in domestic wastewater).

## Slide 14
Chart: Accumulative volume (L)
| 0.2 | 1.2 | 2.2000000000000002 | 3.2
TSS | 2760 | 780 | 470 | 225
COD | 320 | 129 | 124 | 81
TkN | 25.5 | 1.9 | 1.8 | 0.7
Time-course measurement of the selected contaminants concentrations
in the collected storm water

## Slide 15: Outline
Background
Stormwater Infiltration System
Filter design and performance
  Contamination levels in first flush
  Filter design and test

## Slide 16: Filter design consideration
Materials
Hydraulic capacity
Cost
Configuration
Compact
Mechanism
Physical/chemical
Biological
Locally availability
Easy to modify/change
Versatile
Goal: The designed filter module could be implemented to the stormwater drain to
remove contaminants from the “first flush” of stormwater.

## Slide 17: Configuration---- remove contaminants from the first flush
Commercial storm drain filter
(sediment and debris)
Passive flow
(overflow- clean)

## Slide 18
Goal: Alleviate the clogging potential and increase the hydraulic capacity of the system.
Explore alternative filtration materials with higher porosity and bigger particle size.
Gravel
Marble Chip
Zeolite
Biochar
Most common filtration material.
Wide accessibility and low cost.
Recycled material from industrial waste.
Majorly composed with CaCO3.
Provide extra alkalinity.
Aluminosilicate mineral.
Strong cation exchange. capacity (NH4+ removal).
Carbon-enriched biomaterial.
Strong adsorption capacity.
High specific surface area.
Facilitate better nitrification performance in column experiments.
Low mechanical strength.
Filtration Materials
This work was supported by New York State Center for Clean Water Technology (CCWT)

## Slide 19
Packing Media | Size (mm) | Porosity | Nitrogen Loading Rate (NLR, g N m-2 d-1) | NH4+Removal Rate (g N m-1 d-1) | NH4+ Removal Efficiency (%) | Construction Cost ($/m3 nitrification chamber)
Gravel | 10 - 20 | 0.5 | 11.5 - 700 | 11 – 420 | 63 - 95 | 22 - 46
Zeolite | 3 - 6 | 0.4 - 0.5 | 6 - 50 | 5.8 - 36 | 72 - 92 | 80 - 140
Biochar | 5 - 10 | 0.5 - 0.7 | 37.5 - 700 | 35.6 - 560 | 60 - 95 | 210 - 360
Marble Chip | 5 - 20 | 0.5 – 0.6 | 0.6 – 2.4 | 0.5 – 2.3 | 93 – 95 | 63 - 97
Sand | 0.6 - 1 | 0.4 | 1.1 - 8.6 | 0.7 - 8.2 | 80 - 99 | 17.4
Filtration Materials Comparisons
based on N removal and cost

## Slide 20
A
B
C
D
Column | Filling Material | Description
A | Sand | Control group for entire experiment
B | 5 cm gravel (upper) + 10 cm sand (lower) | Reduce the clogging potential of pure sand filter
C | 50 % marble chip (vol) + 50% gravel (vol) | Similar set-up with zeolite + gravel column
D | 50% zeolite (vol) + 50% gravel (vol) | Reduce the time to reach adsorption capacity for NH4+
Selection of Major Filtration Material
Experiment Design

## Slide 21
Wastewater Research & Innovation Facility
Pilot-testing facility that receives domestic wastewater & stormwater
https://www.stonybrook.edu/cleanwater/

## Slide 22
Stage | Description | HLR (gallons d-1 ft-2) | HRT (hours)
1a | Start up columns with same HLR | 12 | 5.2
1b | Test the filter performance at higher HLR | 16 | 3.9
N species: NH4+, NOx-, TKN
Alkalinity
pH
temperature
Diluted Domestic Wastewater (initial N level ~ in stormwater)
sand
10 cm
sand
5 cm
gravel
50%
marble chip
+
50% gravel
50%
zeolite
+
50% gravel
Experimental Design
Selection of Major Filtration Material
15 cm

## Slide 23
Lower NH4+ Levels were observed in zeolite and marble chip columns.
Nitrification (87%) was the major NH4+ removal mechanism of zeolite.
Treatment Performance
Selection of Major Filtration Material

## Slide 24
Sand column and gravel amended column: clogged every 1-2 weeks.
Marble chip amended column and zeolite amended column: no clogging issue.
Hydraulic Performance
Selection of Major Filtration Material

## Slide 25
Zeolite
Zeolite
+
30% Biochar
Marble Chip
+
30% Biochar
Marble Chip
Experimental Design
Stage | Description | HLR (gallons d-1 ft-2) | HRT (hours)
2a | Start up columns with highest HLR tested at stage 1 | 16 | 3.9
2b | Test the impact of biochar amendment at lower HLR (higher HRT) | 12 | 5.2
Impact of Biochar Amendment

## Slide 26
Column | NH4+-N Concentration (mg N L-1) | 
 | Stage 2a | Stage 2b
Influent | 16.2 ± 1.8 | 17.0 ± 2.0
Zeolite | 2.6 ± 1.3 | 1.0 ± 0.3
Zeolite + Biochar | 2.6 ± 1.2 | 1.0 ± 0.5
Marble Chip | 6.3 ± 1.7 | 5.1 ± 1.9
Marble Chip + Biochar | 4.9 ± 1.6 | 3.6 ± 1.2
Impact of Biochar Amendment
Treatment Performance
Increased NH4+ removal was observed in biochar amended marble chip columns, while no significant change was observed in biochar amended zeolite column.
Extended HRT didn’t change the treatment performance of biochar amended columns.
HRT 3.9 hr
HRT 5.2 hr

## Slide 27: Summary and Next Steps
Zeolite and marble chip columns (with bigger particle size and higher porosity) could overcome the hydraulic challenge (12– 16 gallons d-1 ft-2) while similar or better NH4+ removal performance (83.9 – 94.1%)was achieved.
Increased NH4+ removal performance was observed in biochar amended marble chip columns, while no significant change was observed in biochar amended zeolite column.
Optimize and pilot-testing filter media combination to remove a suite of contaminants in the first-flush of stormwater.
Optimize the storm-drain filter configuration design and field-testing with identified sites.
To follow up: xinwei.mao@stonybrook.edu